## Slide 2: Pilkington Austria
Value-Added Products

## Slide 3: Short introduction
Michael Lackner
Product Manager
Pilkington Austria GmbH
Werksgelände 24
A-5500 Bischofshofen
M: +43 664 1603735
E: michael.lackner@at.nsg.com
W: www.pilkington.at
Pilkington Austria image video:
https://www.youtube.com/watch?v=BChh_vaUQoI&t=2s

## Slide 4: Pilkington MirroView™
Transparent mirror for digital applications

## Slide 5: Pilkington MirroView™
Product description:
  Pyrolytic, highly-reflective mirror coating
  Electrically not conductive (compatible w/ PCAP touch)
  Application as a mirror with hidden display
  Suitable for commercial and private use
Function:
  OFF ON

## Slide 6: Pilkington MirroView™
Product family consisting of:
  Pilkington MirroView™
  Pilkington MirroView™ 50/50
Technical data:
Product | Thickness (mm) | Subs-trate | Light trans-mission (%) | Reflexion coating side (%) | Reflexion glass side (%)
Pilkington MirroView™ | 4 | Clear | 25 | 65 | 60
 | 6 | Clear | 25 | 65 | 59
Pilkington MirroView™ 50/50 | 6 | Clear | 35 | 53 | 48
We recommend Pilkington MirroView™ to our customers!

## Slide 7: Applications
Hotels und reception areas
Retail and changing rooms
Banks
Fitness studios
Gastronomy
Bathrooms

## Slide 8: Hotels and reception areas

## Slide 9: Retail and changing rooms

## Slide 10: Banks

## Slide 11: Gastronomy

## Slide 12: Fitness studios

## Slide 13: Bathrooms

## Slide 14: Pilkington MirroView™ Smart
Versatile. Esthetic. Smart.

## Slide 15: Pilkington MirroView™ Smart
Smart Mirror developed by Pilkington Austria
Pilkington MirroView™ 6 mm, toughened, part enamelled
Public Info Display (43” to 75” models available)
High light output (700 cd/m2), 24/7 operation
Optionally available:
  Frame for wall-mounting
  PCAP touch screen
  Remote maintenance service
  SmartFeedback system (SW)

## Slide 16: Customizations and services
Pilkington MirroView™ Smart adjustments:
  Glass dimension (width and height)
  Part enamelling area
  Number and size of the display(s)
  Positioning of the display(s)
Additional services available:
  Planning, installation, commissioning and maintenance
  Consulting and creation of multimedia content
Right product, right place!

## Slide 17: Pilkington MirroView™ Smart
Available Public Info Displays:
Screen diagonal (inches) | Resolution | Aspect ratio | Dimensions W x H x D (mm) | Brightness (cd/m2) | Contrast ratio
43“ (Full HD) | 1920 x 1080 | 16:9 | 960 x 550 x 30 | 700 | 3000:1
49“ (Full HD) | 1920 x 1080 | 16:9 | 1093 x 625 x 30 | 700 | 4000:1
55“ (Full HD) | 1920 x 1080 | 16:9 | 1228 x 701 x 30 | 700 | 5000:1
43” (4K) | 3840 x 2160 | 16:9 | 968 x 558 x 48 | 500 | 4000:1
49” (4K) | 3840 x 2160 | 16:9 | 1099 x 632 x 46 | 500 | 4000:1
55“ (4K) | 3840 x 2160 | 16:9 | 1235 x 708 x 46 | 500 | 4000:1
65“ (4K) | 3840 x 2160 | 16:9 | 1454 x 831 x 46 | 500 | 4000:1
75” (4K) | 3840 x 2160 | 16:9 | 1681 x 960 x 50 | 500 | 4000:1
Watch Pilkington MirroView™ Smart on Youtube!

## Slide 18: SmartFeedback Demo

## Slide 19: Pilkington ViewControl™
Switchable. Multifunctional. Private.

## Slide 20: Pilkington ViewControl™
Switchable glass at push of a button
Switches from opaque to transparent
  OFF mode: opaque
  ON mode: transparent
PDLC film (Polymer Dispersed Liquid Crystal)
Glass structure:
  Pilkington Optiwhite™ toughened/heat strengthened
  EVA film – PDLC film – EVA film
  Pilkington Optiwhite™ toughened/heat strengthened
Busbars for electrical connection

## Slide 21: Function principle and film structure

## Slide 22: Technical data
Description |  | Mode | Values
Operation mode | Power | ON OFF | Transparent Opaque
Electrical properties | Operating voltage Operating temperature Power consumption Available Power Supplies | ON ON / OFF ON | 60 VAC (50 / 60 Hz) -20 ~ +60 °C 3 - 5 W/m2 60 VAC / 35 W (up to 1,5 m2) 60 VAC / 100 W (up to 5 m2) 80 VAC / 100 W (up to 4,5 m2)
Film properties | Width Length Colour Visible Light Transmittance Haze Switch time Life time | ON OFF ON ON / OFF | Up to 1800 mm Up to 3500 mm White 75 % 55 % 5 % < 0,1 sec > 10 years
Glass properties | Mono glasses Construction |  | Pilkington Optiwhite™ Laminated glass 44.4, 66.4, 88.4 out of toughened / heat strengthened glass
Additional properties | Rear projection Controlling possibilities | OFF | Available Switch, bus connection, remote control

## Slide 23: Busbar alignment

## Slide 24: Applications
Meeting rooms
Mobile partitions
Windows & Doors
Bathrooms
Hospitals
Back projections

## Slide 25: Demo

## Slide 26: Pilkington DesignPrint
Aesthetic. Individually. Resistant.

## Slide 27: Construction of print heads

## Slide 28: Colour system

## Slide 29: Digital printer – drop sizes
7 different drop sizes
Smaller drop sizes -- better resolution
Bigger drop sizes -- higher opaqueness

## Slide 30: Technical data
Glass thicknesses: From 4 to 19 mm
Maximum glass sizes: From 200 x 300 mm, to 2500 x 4500 mm
Resolutions: From 360 to 1440 dpi
Supported file formats: PDF, CDR, AI, BMP, PSD, TIFF, JPEG, GIF, PNG
Translucency: Colour gradients and graduations possible
Special colours: Etching-, transparent- and metallic effect, non-slip-, gold and platinum colours
Compliances All colours are RoHS compliant
Resistances: Colours can be used on layer 1

## Slide 31: Pilkington Suncool™ Dynamic
Easy. Dynamic. Maintenance-free.

## Slide 32: Pilkington Suncool™ Dynamic

## Slide 33: Pilkington Suncool™ Dynamic
People should feel comfortable in their homes
How can glass contribute?
  Light transmission
  Thermal insulation
  Sun protection
  Optics and aesthetics
But: most glasses are static, but not the weather!
Idea: Adaptive glass!

## Slide 34: What is Pilkington Suncool™ Dynamic?
Pilkington Suncool™ Dynamic
  Thermochromic laminated safety glass *!
Thermochromic:
  Change in the transmission of solar radiation as a function of the glass transition temperature
* according to Din EN 14449, laminated safety glass out of heat strengthened glass

## Slide 35: Basic idea
Strong sunlight  high absorption  high glass temperature  strong tinting
Low temperature  low absorption  low glass temperature  no tinting

## Slide 36: Technical data
Product | Form | Light transmission, TL (%) | Solar heat gain coefficient, g-value (%)
Pilkington Suncool™ Dynamic Mono (laminated safety glass) | clear | 62 | 67
 | tinted | 10 | 44
Pilkington Suncool™ Dynamic double IGU – Ug value 1,1 | clear | 56 | 46
 | tinted | 9 | 21
Pilkington Suncool™ Dynamic double IGU – Ug value 1,0 | clear | 48 | 34
 | tinted | 8 | 14
Pilkington Suncool™ Dynamic triple IGU – Ug value 0,7 | clear | 51 | 39
 | tinted | 9 | 16
Pilkington Suncool™ Dynamic 9.2 mm meets the impact test requirements of EN 12600 (pendulum test 1B1)

## Slide 37: Advantages
Adapted sunscreen at any time of the year or day
No electricity
Maintenance-free
Automatic tinting
Reduced glare
UV protection (protects against fading)
Advantages over static glass

## Slide 38: Combination possibilities
Pilkington Optitherm™
  Thermal insulation
Pilkington OptiView™
  Anti-reflection
Pilkington Suncool™
  Additional sunscreen
Pilkington Activ™
  Self-cleaning
Right product, right place.

## Slide 39: Availability
Pilkington Suncool™ Dynamic from toughened float glass:
  9,2 mm laminated: 1638 x 2850 mm
  11,2 mm laminated: 1638 x 3000 mm
  13,2 mm laminated: 1638 x 4000 mm
  17,2 mm laminated: 1638 x 4000 mm
Pilkington Suncool™ Dynamic from heat-strengthened float glass:
  9,2 mm laminated: 1638 x 2500 mm
  11,2 mm laminated: 1638 x 3000 mm
  13,2 mm laminated: 1638 x 4000 mm
  17,2 mm laminated: 1638 x 4000 mm
Weight limit:
  Max. 250 kg per mono glass
  Max. 500 kg per laminated glass

## Slide 40: Pilkington Mirropane™ Chrome
Esthetic. Safe. Durable.

## Slide 41: Pilkington Mirropane™ Chrome